## Slide 1
Metallic magnetic calorimeters for
high resolution
x-ray and particle detection
A.Fleischmann, L.Gastaldo, D.Hengstler, S.Heuser, A.Kampkötter, C.Pies, J.P.Porst, S.Kempf, S.Schäfer, P.Ranitzsch, C.Enss
Kirchhoff Institute for Physics Heidelberg University

## Slide 2: detection principle of micro-calorimeters
Operation at low temperature (T < 0.1 K):
small specific heat
large temperature change
small thermal noise
Temperature change
Relaxation to bath temperature
Thermal bath (T < 100mK)
Weak thermal link G
Absorber C
Thermometer
X-ray photon

## Slide 3: Metallic Magnetic Calorimeters
paramagnetic sensor: Au:Er
main differences to calorimeters with resistive thermometers
no power dissipation in the sensor
no galvanic contact to the sensor
signal size:
M
T

## Slide 4: readout of magnetic calorimeters
two-stage SQUID setup with flux locked loop to linearize the first stage SQUID
allows for:
T = 50 mK
T = 0.5 ... 4 K
room temperature
Detector
Amplifier
low noise
large bandwidth / slewrate
small power dissipation on detector SQUID chip (voltage bias)
paramagnetic sensor
SQUID
magnetometer

## Slide 5: sensor and pickup coil geometries
early devices:
cylindrical T-sensor
circular SQUID loop
external magnetic field
present working horse:
planar T-sensor
sc. meander shaped pickup loop
B-field generated by persistent current
transformer coupled to SQUID
just started:
sandwiched planar sensor
best filling factor

## Slide 6: signal size
Au:Er 300 ppm
Inverse Temperature T1 [K 1]
Magnetization M [A/m]
Au:Er 300 ppm
Temperature T [mK]
Specific heat C [104 J mol1K1]
Au:Er 300 ppm
thermodynamic properties of interacting spins (RKKY) can be calculated with confidence by mean field approximations
Signal size of a detector can be calculated with confidence

## Slide 7: noise contributions
Cabs
fluctuations of energy between sub-systems
(optimum for Cabs = Cspins)
flux noise of SQUID-magnetometer
SF = 2 e L, required:
magnetic Johnson noise
- thermal currents in the metallic components
- marginal in all present detectors
excess 1/f noise SF ~ NEr
SF ~ 1/f, Sm|1Hz ≈ 0.023 mEr2/Hz
temperature independent (20mK – 4K)
sensor
SQUID
Cspins

## Slide 8: expected energy resolution for some configurations
Absorber [mm3] | Cabs [pJ/K] @ 50mK | t1 [ms] | DEFWHM [eV] @ 50 mK | DEFWHM [eV] @ 30 mK
250  250  5 (Au) | 1 | 1 | 2.2 | 1.2
250  250  5 (Au/Bi) | 0.3 | 1 | 1.1 | 0.6
 | 0.3 | 0.3 | 1.5 | 0.8
1000  1000  200 (Au) | 500 | 1 | 50 | 25
meander geometry
signal rise time: t0 < 1 ms
thermodynamic fluctuations of energy
1/f noise of Er ions
flux noise of SQUID
    white: SF = 0.5 mF0/Hz
    1/f: SF = 5 mF0/Hz @ 1Hz
realistic flux coupling to a 1.6 nH current sensor SQUID (PTB)
considering:

## Slide 9: Detectors for a veriety of applications

## Slide 10: maXs-20: detector arrays for x-rays up to 20 keV
first array prototype:
1x8 x-ray absorbers
250 mm  250 mm  5 mm gold
98% quantum efficiency at 6 keV
DEFWHM < 3 eV

## Slide 11: maXs-20: detector arrays for x-rays up to 20 keV
present system for HD-EBIT
pulse-tube cooled ADR
Base 27 mK
Time below 30mK: 24h

## Slide 12: micro-fabrication of x-ray detectors
niobium meanders:
width 3 - 5 mm
thickness 400 nm
critical current 250 mA
2 x higher than required for optimum performance
no additional flux noise when charged
on-chip persistent current switch:
heater: sputtered AuPd
R = 20 W
switching current 1 – 2 mA
reliable injection of persistent currents up to 0.95 Ic

## Slide 13: micro-fabrication of x-ray detectors
sputtered Au:Er T-sensors:
1 - 3 mm thick
co-sputtered from Au and Au:166Er targets
Since recently:
Magnetization and specific heat agree almost perfect with bulk values

## Slide 14: micro-fabrication of x-ray detectors
overhanging x-ray absorbers:
5 mm thick gold, RRR ≈ 15
electroplated into photoresist mold
connected to sensor through stems to reduce loss of initial energetic phonons to the solid substrate
effective contact area: < 5% of absorber area

## Slide 15: signal rise-time of micro-fabricated MMCs
rise time: 90 ns @ 30 mK,
as expected for the electron-spin-relaxation from Korringa-constant for Er in Au

## Slide 16: micro-fabrication of x-ray detectors
metallic thermal link to the bath:
sputtered Au film to adjust decay time
here: 1 ms – 3 ms
nearly single exponential decay
thermal bath
thermal bath

## Slide 17: maXs-20: detector arrays for x-rays up to 20 keV
characterization with an 55Fe-source
designed energy resolution of DEFWHM = 2.5 eV
slightly spoiled by increased stray inductance (~ nH)
DEFWHM = 3.4 eV @ 6 keV
DEFWHM = 3.0 eV @ 0 keV
Un-triggered noise:

## Slide 18: New: „sandwiched“ sensor for improved flux coupling
Planar spiral pickup coil
Sensor sandwiched between spiral and sc. top plane
Magnetic filling factor close to unity
close to best flux coupling

## Slide 19: New: „sandwiched“ sensor for improved flux coupling
First prototype
1 pixel
absorber: 5mm thick gold,  150mm
signal decay time < 1 ms
defined by metallic link to thermal bath

## Slide 20: New: „sandwiched“ sensor for improved flux coupling
First characterization with an 55Fe-source
DEFWHM = 2.0 eV @ 6 keV
DEFWHM = 1.8 eV @ 0 keV
55Mn
Energy resolution will be pushed below DEFWHM = 1.4 eV
by further reducing
stray inductances
some excess heat capacity
stem area to further reduce loss of athermal phonons

## Slide 21: maXs-200: detector arrays for hard x-rays (at GSI/FAIR)
First array prototype
1x8 x-ray absorbers
2 mm x 0.5 mm
200 mm thick electroplated Au
80% QE at 100 keV
DEFWHM < 50 eV
4 electronic channels
modular extension to longer arrays
photo resist mold
electroplated Au absorbers

## Slide 22: maXs-200: detector arrays for hard x-rays (at GSI/FAIR)
First characterization with an 241Am-source
DEFWHM = 60 eV @ 60 keV
DEFWHM = 40 eV @ 0-10 keV
237Np
Slight degradation towards higher energies due to
Poor temperature stability in this first experiment
Possible marginal position dependence, to be fixed by stems between absorber and sensor

## Slide 23: linearity of maXs-200
Non-linearity at 60 keV
0.1 %

## Slide 24: large area MMC with position and energy sensitivity
For the detection of neutral molecular reaction products
at the cryogenic ion storage ring MPI-K, HD
(e.g. dissotiative recombination)
detector:
36 mm in diameter
16 absorber segments
16 temperature sensors
energy resolution 100eV – 200 eV
position resolution 200 mm – 1mm

## Slide 25: large area MMC with position and energy sensitivity
pulse area → energy
rise time → position

## Slide 26: large area MMC with position and energy sensitivity
micro-fabricated large area detector
absorbers supported by 200 micron-sized stems
wrinkles to reduce thermal stress

## Slide 27: large area MMC with position and energy sensitivity
signal
signal
Time [ms]
Time [ms]
First test with LED light pulses
Position dependence of signal shape
agrees perfectly with numerical FEM simulation
glass fibers

## Slide 28: New: m-calorimeters with magnetic penetration thermometers (MPT)
Replace paramagnetic temperature sensor by superconductor with low Tc (e.g.100mK)
Has all good properties of metallic magnetic calorimeters
    No intrinsic power dissipation
    No galvanic contact to sensor
    Wide range of operational temperatures
    Fast
Plus:
    Larger signal size due to larger a = d logF / d logT
      Reduced read out noise requirements
    Easier access to low heat capacity devices for UV and IR
First test devices: DEFWHM = 15 eV, bulk Hf sensor (Heidelberg)
DEFWHM = 4 eV, MoAu bi-layer (NASA GSFC)
Use T-dependent B-field penetration as thermometer
Very promising!
&

## Slide 29: Multiplexed read-out of detector arrays
each MMC coupled to an un-shunted single junction SQUID
flux change de-tunes the resonance of a coplanar l/4 resonantor (4-8 GHz)
single HEMT amplifier and 2 coaxes to read out 1000 detectors
Microwave SQUID multiplexing (K. Irwin, NIST)

## Slide 30: summary & outlook
metallic magnetic calorimeters
suitable for high-res x-ray spectroscopy
versatile low temperature detectors
can cover wide range of applications
micro-farbrication works
first detector arrays fabricated
material properties close to bulk values
expected performance will be reached
next steps
demonstration of multiplexed read-out to increase channel-count significantly
for AMoRE
we are happy to provide existing devices and support the development of dedicated ones

## Slide 31: Detectors for a veriety of applications

## Slide 32: calorimeteric detectors are ...
... a quite dull technique to detect photons
(photon converted to heat)
... bad detectors at room temperature
... a canonical ensemble
→ energy content fluctuates
e.g.
1 cm3 of Ge at 300K: DEFWHM ≈ 1 GeV
at 50mK: DEFWHM ≈ 1 eV
Thermal bath (T < 100mK)
Weak thermal link
Absorber C
Thermometer
X-ray photon
Important: Fast internal thermalization !
→ normal metal absorbers (but: higher specific heat)
→ typ. volume < mm3

## Slide 33: linearity
 1 %
Measured energy E [keV]
Photon energy E [keV]
DE [eV]
Typical non-linearity:
1-3% at 6 keV