## Slide 1: Discussion & Summary
Sun Kee Kim
Seoul National University
2nd AMoRE Workshop, Kiev, Oct. 27-28, 2011

## Slide 2
Goal of the workshop
Review of the current status
Identify the issues for the crystal growing/ purification of materials
Identify the issues for the 1st stage experiment
Decide whether we have 2nd stage : cryogenic detector w/ about 5kg mass CMO
Identify the issues for the 100 kg detector design
List of tasks
…
Discussions on
Job sharing
Collaboration issue ?
Steering committee  Institutional board ?
…

## Slide 3
Issues on Crystal growing
Specification on crystals
  Background index
  Transparency
  Light yield
  Size & shape
Quick feedback mechanism needed ?
Specification for ISTC project exists
Good time to update the specification
Some known but not understood issues
  Recrystallization reduces background, but degrade the light yield?
    Background reduction factor ?
    Can we use natural materials for this study?
  How to improve the current enriched crystals?
    Enriched crystals at Y2L ~ 850 g
    The rest at FOMOS  we need to decide what to do
    Special issue is on recovery of enriched material from the waste
    Loss of material/effort/cost/etc on the waste recovery should be understood

1) How many recrystallization processes can be done (seems to be even one is questionable because evaporation of Mo and broken stoichiometry);
2) One should check ZrO2 ceramics (as possible very radioactive)
3) Is it possible to replace (seems to possible, but need an R&D to choose crystal growth conditions because different thermo properties of ZrO2 and e.g. alumina);
4) What is segregation coefficient for Th (which the most dangerous for AMoRE)? I expect 0.3 from our study of CaWO4 [NIMA 631 (2011) 44];
5) Protocol to obtain a certain level of purity in powder is strongly requested; 6) recovery of 48Ca and 100Mo obviously is needed. We could propose our experience (Dr. Roman Boiko) to develop such a technique. Questions by Fedor Danevich look the F.Danevich’s talk

## Slide 4: ISTC3293 (2006.3-2007.5)
Expected results:
- Requests on optimum geometry, light output and transparency of СаМоО4 crystals, and also tolerable content of dangerous radionuclides in crystals to get a sensitivity of the experiment of 1025 years.
- Technology of big volume СаМоО4 crystal growing of high quality (with diameter up to 45 mm and length of up 240 mm). Light output of the crystals under room temperature 2500 photons/MeV; scintillation kinetics up to 0.1 ms in the range of temperature of 77-293K.
- Radiopurity of the crystals grown of raw material of high purity (using specially developed technology of purification) should be satisfied of request of the double beta decay experiment at YangYang laboratory in Korea, namely  20 Bq/kg of 214Bi and 208Tl (238U and 232Th series).

## Slide 5
Issues on Cryogenic 100 kg detector
Experiment design
  Crystal geometry:
    size and shape
    Photon detection scheme
    Packing
    cables
  Sielding and Cryostat
  Space
Need an organized effort
R&D issues
  Improvement of energy resolution for large crystal
  Photon detector development
  Thermal modeling
  Position information ?
  Pulse shape information ?


## Slide 6: How about…
Workgroups
Role : identify issues and make a list of works
Material purification and Crystal
1st stage experiment
Cryogenic detector
Simulation

## Slide 7
Next AMoRE Collaboration meeting ?