## Slide 1: Goal of the workshop
Sun Kee Kim
Seoul National University
2nd AMoRE Workshop, Kiev, Oct. 27, 2011

## Slide 2: Amore Collaboration
Korea (39)
Seoul National University : H.Bhang, S.Choi, M.J.Kim, S.K.Kim, M.J.Lee, S.S.Myung, S.Olsen, Y. Sato, K.Tanida, S.C.Kim, J.Choi, H.S.Lee, S.J.Lee, J.H.Lee, J.K.Lee, X.Li, J.Li, H.Kang, H.K.Kang, Y.Oh, S.J.Kim, E.H.Kim, K.Tshoo, D.K.Kim(24)
Sejong University : Y.D.Kim, E.-J.Jeon, K. Ma, J.I.Lee, W.Kang, J.Hwa (5)
Kyungpook national University : H.J.Kim, J.So, Gul Rooh, Y.S.Hwang(4)
KRISS : Y.H.Kim, M.K.Lee, H.S.Park, J.H.Kim, J.M.Lee, K.B.Lee (6)
Russia (16)
ITEP(Institute for Theoretical and Experimental Physics) : V.Kornoukhov, P. Ploz, N.Khanbekov (3)
Baksan National Observatory : A.Ganggapshev, A.Gezhaev, V.Gurentsov, V.Kuzminov, V.Kazalov, O.Mineev, S.Panasenko, S.Ratkevich, A.Verensnikova, S.Yakimenko, N.Yershov, K.Efendiev, Y.Gabriljuk (13)
Ukraine(11)
INR(Institute for Nuclear Research) : F.Danevich, V.Tretyak, V.Kobychev, A.Nikolaiko, D.Poda, R.Boiko, R.Podviianiuk, S.Nagorny, O.Polischuk, V.Kudovbenko, D.Chernyak(11)
China(3)
Tsinghua University : J.Li, Y. Li, Q.Yue(3)
Germany(3)
University of Heidelberg : C.Enss, A. Fleischmann, L. Gastaldo (3)
5 countries
9 institutions
72 collaborators

## Slide 3
Y2L
Located in a tunnel of
Yangyang Pumped Storage Power Plant
Korea Middleland Power Co.
Minimum vertical depth : 700 m
Access to the lab by car (~2km)
In operation since 2003
Experiments:
KIMS: DM search exp. in operation
AMORE: DBD Search exp. in preparation
(additional laboratory space in design)
YangYang Underground Laboratory(Y2L)
(Upper Dam)
(Lower Dam)
(Power Plant)

## Slide 4
~500 p.e./MeV
20kg

## Slide 5: CaMoO4 crystal development

## Slide 6
ISTC program
Ukraine-Korea program

## Slide 7
2009.10.15-10.17 1st workshop – Collaboration formed (needs of a body for decisions)
Steering committee : S.K.Kim, Y.D.Kim, H.J.Kim, Y.H.Kim, V. Kornoukhov, F. Danevich
2010.3.16 : Collaboration name AMoRE was decided
2010. 5. 7 : AMoRE software workshop
2010.10.7 : 2nd workshop
2011.10.27 : 3rd workshop (today)
INDICO Documents archive for AMORE
http://q2c.snu.ac.kr/indico/categoryDisplay.py?categId=16
Presentation files for 1st workshop
http://q2c.snu.ac.kr/indico/conferenceDisplay.py?confId=11
For 2nd workshop
http://q2c.snu.ac.kr/indico/conferenceDisplay.py?confId=70
Need a beautiful logo of AMoRE

## Slide 8
Recent presentations (this year)
MEDEX 2011 (2011.7.13-16) (invited)
ASPERA Workshop on The next generation projects in Deep Underground Laboratories (2011.7.29-8.2) (invited)
LTD 2011(2011.8.1-5)
TAUP 2011(2011.9.5-9)
SCINT 2011(2011.9.12-16)
DBD 11(2011.14-17) Osaka (invited)
Recent publications
The Development of a Cryogenic Detector with CaMoO4 Crystals for Neutrinoless Double Beta Decay Search Astroparticle Physics, 34, 732 (2011)
Neutrino-Less Double Beta Decay Experiment Using Ca MoO Scintillation Crystals, IEEE Trans. Nucl. Sci. 57, 3 (2010)
Ancient Greek lead findings in Ukraine, Nucl. Inst. Meth.A 603, 328, (2009)
Development of CaMoO4 crystal scintillators for a double beta decay experiment with 100Mo, Nucl. Inst. Meth. A 584, 334 (2008)
AMoRE

## Slide 9: 0νββ
1/T0ν 1/2 = G0ν(Q,Z) |M0ν|2 <mββ>2
Transition bb
allowed
Forbidden  transition
Z
Energy
Z
Z+1
Z+2
Qbb
100Mo
100Ru
100Tc

## Slide 10
Werner Rodejohann, Int. J. M. Phys., 2011

## Slide 11: CaMoO4
DBD for Mo-100 (3034 keV), Ca-48(4272 keV)
high energy  less background
Mo-100 enrichment >90% not so difficult
for Mo-100 search, Ca-48 needs to be depleted
Scintillator
  At room temp; 10-20% of CsI(Tl) at 20o
  Decay time ; 16 μ sec
  LY increases at lower temp. (almost the same as CsI(Tl))
  Wavelength; 450-650ns-> RbCs PMT or APD
  Pulse Shape Discrimination
Can be used as cryogenic detector
  Debye temperature: 438 K ( Ge : 360 K, Si: 625 K)
  Combining with Scintillation detection : NR, alpha/gamma separation
  Good dark matter detector as well
Z
Energy
Z
Z+1
Z+2
Qbb
100Mo
100Ru
100Tc

## Slide 12: Enrichment & Depletion
Mo-100 enrichemeinet : 96.1%
Ca-48 depletion < 0.001% (Nantural abundance is 0.187%)
Depleted Ca : ~ 30 kg available (Ca48 < 0.001%)
 Good for 150 kg CaMooO4 crystals

## Slide 13: 48Ca Enrichment/Depletion at KAERI (Korea Atomic Energy Research Institute)
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
RPI
(-) Charge collector
target isotope
other isotope
target isotope ion
Atomic vapor
ISOP
ALSIS (Advanced Laser Stable Isotope Separation)
- Features : Isotope-Selective Optical Pumping (ISOP)
followed by Non-selective Resonant Photoionization (RPI)
- ISOP gives good isotope-selectivity and non-selective RPI high yield.

## Slide 14: Performance of CMO+MMC
FWHM = 11.2 keV
42 keV
FWHM = 1.7 keV
Emission line of Mo : 18keV
Astropart. Phys.34, 732, 2011
5.5 MeV alpha
60keV gamma
high energy resolution
suitable to search for Mo-100 0νββ
low energy thresold
suitable to search for WIMP

## Slide 15
Cryogenic CaMoO4 Sensitivity
0.5% FWHM 15 keV FWHM for low temp.
5 years, 100 kg 40Ca100MoO4 : T1/2 = 3.0x1026 years  <m> = 20 – 70 meV
Fully covers
inverted hierarchy
CaMoO4
Eth=10 keV (5 and 100 kg year)
CaMoO4
Eth=1 keV
(5 and 100 kg year)
XENON100 6000 kgd
SuperCDMS 25kg
Hirsch et al, PLB679:454-459,2009
Dark matter search
 High sensitivity

## Slide 16
From V. Kornoukhov

## Slide 17
1) SB28 40Ca100MoO4 crystal.
It was grown 09.09.2009.
H = 25,5 mm,
Dmax = 49,5 mm
Dmin = 40,5 mm
Mass = 195,94 gr.
Annealing procedure into oxygen atmosphere = 312 hours.
Colourless. There is weak blueness along small diameter of the ellipse.
The end face of the crystal was polished to optical grade quality.
Note. To accelerate annealing procedure, the cylinder side of the crystal was grinded with the sand paper 600/800 grade.
2) SB29 40Ca100MoO4 crystal.
It was grown 11.09.2009.
H = 48/51 mm,
Dmax = 50,0 mm
Dmin = 42,5 mm
Mass = 390,35 gr.
Annealing procedure into oxygen atmosphere = 240 hours.
Colourless. There is weak blueness along small diameter of the ellipse.
The end face of the crystal was polished to optical grade quality.
Note. No grinding of the cylinder side of the crystal was done.
40Ca100MoO4

## Slide 18: 40Ca100MoO4
S35
SB28
CMO-3
D44 mm x L51 mm
~ 300g

## Slide 19: Light output of SB35
SB35
Resolution : 16% (FWHM)
Mean : 5.97 x 105
CMO_3
Resolution : 16% (FWHM)
Mean : 6.79 x 105
SB28
Resolution : 30% (FWHM)
Mean : 2.88 x 105

## Slide 20: Experimental setup at Y2L
CsI detectors surround the CaMoO4 crystal
511keV signal is a opposite direction for momentum conservation.
(back to back cut)
CaMoO4 is surrounded by 14 CsI crystals & 14 PMTs.
CsI CaMoO4
  6.5x5.5x30cm(12) - 2.2x2.2x6cm (2)
  9x9x6cm(#13 & #14) - 255g
PMTs & CsI crystals are crossly connected.
Lead shielding(10 cm)
Add more PMTs soon

## Slide 21
1st stage experiment (pilot experiment)
0.5-5kg CMO crystal
Scintillation only
 J.H.So

## Slide 22: Detector installation - Ruslan
Mineral Oil
Teflon wrapping

## Slide 23
CANBERRA HPGe
Auto-filling system installed
Lower background level than the previous one
Mo-92 EC beta+ experiment will be done
Background control of AMoRE material selection
 YDKim’s talk
Notes: Three days ago, We was replace a ortec hpge with new canberra detector.
So, This is picture for new canberra detector
The left picture is before assembly and The right picture is after assembly

## Slide 24
1st stage experiment (up to ~5 kg ?)
-- should be carried out within the currently available budget.
Intermediate step could be
5kg Cryogenic detector
(maybe possible w/o additional funding)
100 kg Cryogenic detector  We should aim for it
will need new budget
funding opportunity exists!
 Design of the experiment should be done

## Slide 25
National Facility Road Map (NFRM)
Included in a list of 71 out of 282 proposals

## Slide 26: Toward 100 kg Cryogenic detector
241Am source
teflon-coated
copper springs
thermalization pad
(gold film)
meander MMC
4cm (D) x 4cm (L) ~ 211g
Issues :
Energy resolution improvement
module size
photon detector
readout channels  multiplexing ?
cryostat, shielding

## Slide 27
CUORE
90 cm d x 100 cm h
TeO2 +
Ge NTD sensor
10 mK
2700 wires
shield 30 cm Pb
cryogen-free
cooling power
1.5mW at 120 mK
6 μW at 10 mK
Cryostat

## Slide 28
First guess :
100 kg CaMoO4
density : 4.2g/cm3
30cm d x 33cm h ~ 100 kg
Cooling power : 650 ㎼ at 120mK
Cryostat

## Slide 29
Report by Li Jin, Aug. 2011

## Slide 30
Inner lead shield
Report by Li Jin, Aug. 2011

## Slide 31
Report by Li Jin, Aug. 2011

## Slide 32
Goal of the workshop
Review of the current status
Identify the issues for the crystal growing/ purification of materials
Identify the issues for the 1st stage experiment
Decide whether we have 2nd stage : cryogenic detector w/ about 5kg mass CMO
Identify the issues for the 100 kg detector design
List of tasks
…
Discussions on
Job sharing
Collaboration issue ?
Steering committee  Institutional board ?
…