## Slide 1
3М
reflector
ZnWO4
ZnWO4
ZnWO4
PMT
PMT
PMT
teflon
optical
contact
No optical contact (plex.
cubes)
Measurement of transparency of ZnWO4
V.M.Mokina1, F.A.Danevich1, V.V.Kobychev1, H.Kraus2, V.B.Mikhailik2, L.L.Nagornaya3
1 Institute for Nuclear Research, MSP 03680 Kyiv, Ukraine
2 University of Oxford, Department of Physics, Keble Road, Oxford OX1 3RH, UK
3 Institute for Single Crystals, 61001 Kharkiv, Ukraine
Optimization of light collection from crystal scintillators to search for dark matter and 2 decay
Light output and energy resolution for dark matter and 2 decay are important:
Energy resolution and relative pulse amplitude for 662 keV 137Cs
Energy resolution and relative pulse amplitude for 662 keV 137Cs
Energy resolution and relative pulse amplitude in conditions similar to scintillation bolometers
Preliminary simulation of relative pulse amplitude by ZEMAX
Conclusions
Best energy resolution and relative pulse amplitude was measured for hexagonal crystal with diffused side and top surfaces, optical contact and 3М reflector;
In measurement without optical contact (condition of scintillating bolometer) best relative pulse amplitude was registered with hexagonal crystal, diffused side and polished top surfaces, and 3M reflector around the crystal with the air gap with thickness 5 mm between ;
Previous results of simulation by ZEMAX reasonably describe the experimental data. The simulation by GEANT4 is in progress now.
Plans
Investigations of other shapes of crystal:
Oval Octahedron
Advantage: minimal lost of initial crystal mass
Experimental
-Lambertian reflection 50
-bulk scattering = 0
Simulation
  1.all surface polished; 2.diffused side surface;
  3.diffused side and top surfaces; 4.all surface diffused
  ZnWO4
  ZnWO4
  1.all surface polished; 2.diffused side surface;
  3.diffused side and top surfaces; 4.all surface diffused
  ZnWO4
Energy spectra of 137Cs and 207Bi
cylinder
hexahedron
Conditions of measurements
Measurement follow with different kind of surface of crystal :
  1. all surface polished; 2. diffused side surface;
  3. diffused side and top surfaces; 4. all surface diffused.
To achieve low energy threshold (most important for dark matter experiments);
To improve energy resolution (2 experiments);
To improve particle discrimination (both for DM and 2 experiments);
Discrimination of random coincidence of
22 events
[D.M. Chernyak et al., Eur. Phys. J. C 72 – 2012 – 1989. ].
Aims of investigation
Optimisation of light collection conditions from crystal scintillators to obtain higher light output and better energy resolution
Influence on energy resolution and light collection:
shape of crystal (hexagonal, cylindrical)
surface (polished, diffused)
type and shape of reflector
presence of optical contact with photo-detector